## Slide 1: Performance of the GAMMA400 Calorimeter Prototype
Vannuccini Elena
On behalf of the GAMMA400 Florence group

## Slide 2: Active material & sensor
CsI(Tl) scintillating crystals
  3.6 cm side (  1 Molière radius )
  Diffusive wrapping (100 m Teflon tape)
Excelitas VTH2090 photodiodes
  Large area (9.29.2mm2)
Density | 4.51 g/cm3
Wavelength @max | 550 nm
Light output | 45 % of NaI(Tl)
Primary decay time | 1 ms

## Slide 3: Crystal wrapping
Teflon
Tyvec
Teflon + Vikuiti
Vikuiti
Studied by comparing signal induced by 5,5 MeV α from Am source
Tested materials:
  Teflon (diffusive)
  Tyvec (diffusive)
  Vikuiti (reflective)
Applied to prototype
  Feb.2013  Teflon
  Feb.2015  Teflon+Tedlar
  Aug.2015  Vikuiti (planned!)

## Slide 4: The calorimeter assembly
4mm gap between active elements
33 elements for each plane
   1.5 RM shower containment
14 layers
  active depth 27 X0  1.44 lI
126 total elements

## Slide 5: Front-end electronics
CASIS chip (developed by INFN-Trieste)
  Very large dynamic range (010000 MIP)
  Automatic switching btw low and high (20) gain mode
  16 channels (CSA+CDS shaper)

## Slide 6: Beam tests
Ion beams extracted from CERN SPS H8 line
  Feb 2013  A/Z=2 ions (12.8 and 30.0 GeV/u) from Pb primary beam on Be target
  Feb 2015  primary Ar and A/Z=2 ions (19.0 and 30.0 GeV/u) from Ar beam on Polyethylene target
ION
BEAM
BEAM TRACKER (BT)
4 Si-pixel matrixes + 8 Si-strip layers
Z tagging
particle tracking (<200m resolution)
CALORIMETER PROTOTYPE
3314 CsI(Tl) crystals

## Slide 7: Beam Tracker (BT)  Z-tagging
8 dE/dx meas. from Si-strips
4 dE/dx meas. from Si-pixels
Courtesy of Siena group

## Slide 8: Beam Tracker (BT)  precise beam position
Central cube first layer
Courtesy of Pisa/Siena group
Equalized ADC counts
X (cm)
Y (cm)
He ions traversing the photodiode
  1MIP(Si)/1MIP(CsI) ~ 3040%

## Slide 9
He @12.8 GeV/u
He @30.0 GeV/u
C @12.8 GeV/u
Na @12.8 GeV/u
0
1
2
3
4
5
6
7
8
9
10
11
12
13
14

## Slide 10: Single crystal performance

## Slide 11: Channel Noise
RMS( PED )
RMS( PED-CN)
CASIS
0
CASIS
1
CASIS
2
CASIS
3
CASIS
4
CASIS
5
CASIS
6
CASIS
7
CASIS
8
ADC counts
Channel pedestals (PED) evaluated by acquiring off-spill events
Random noise (RN)  common noise (CN)  3040 ADC counts

## Slide 12: Single crystal signal
All events
Not-interacting 4He
4He
2H
Test 2013
Pb+Be
30 GeV/u
hig gain | low gain
Signal of the first crystal along the beam direction
log(ADC counts)
Hit  5RN cut

## Slide 13: Single crystal signal
All events
Not-interacting 4He
4He
2H
Test 2015
Ar+Polyethylene
30GeV/u
hig gain | low gain
log(ADC counts)
Signal of the first crystal along the beam direction
Hit  5RN cut

## Slide 14: Gain dispersion
Crystal responses equalized by normalizing to 4MIP the ionization energy deposit of 4He (@peak)
2013 
RMS  14%
ADC counts
1500

## Slide 15: Gain dispersion
(Spare plane with test crystals)
CsI(Tl) with diffusive+reflective wrapping (Teflon+Vikuiti)
RMS  21%
Crystal responses equalized by normalizing to 4MIP the ionization energy deposit of 4He (@peak)
2015 
Lower signal and larger dispersion due to absorber wrapping
ADC counts
1510
1050
(preliminary)

## Slide 16: Test of scintillating materials
Test of 9 scintillating materials
  CsI:Na, CsI:Tl, YAG:Ce, BaF2, YAP:Ce, LuAG:Ce, BSO, BGO, LYSO:Ce
  Teflon+Vikuiti+Tedlar wrapping
Z-tagging from BT+CAL
Study of the ionization signal –vs– Z2
BEAM TRACKER (BT)
4 Si-pixel matrixes + 8 Si-strip layers
CALORIMETER
3314 CsI:Tl crystals
SPARE PLANE
33 test crystals
ION
BEAM

## Slide 17: Test of scintillating materials
 | Expected |  | Measured |  | 
 | Z=1 (a.u.) | Z=2 (a.u.) | Z=2 (ADC counts) | Norm. @CsI:Tl (a.u.) | Measured/Expected
CsI:Na | 43 | 172 | 1336 | 229 | 1,3
CsI:Tl | 100 | 399 | 2330 | 399 | 1,0
YAG:Ce | 19 | 78 | 642 | 110 | 1,4
BaF2 | 10 | 40 | -- | -- | --
YAP:Ce | 16 | 65 | 316 | 54 | 0,8
LuAG:Ce | 11 | 44 | 674 | 115 | 2,6
BSO | 3 | 12 | -- | -- | --
BGO | 11 | 46 | 312 | 53 | 1,2
LYSO:Ce | 38 | 151 | 759 | 130 | 0,9
(preliminary)

## Slide 18: Z resolution
Not-interacting ions
12.8 GeV/u
test 2013
Courtesy of Pisa/Siena group
Good Z separation up to Oxygen

## Slide 19: Ionization signal –vs– Z2
O
|
F
|
Ne
|
Linear fit from He to O
Linear fit from Na to Cl
Na
|
|
Cl
 low
 high gain
Ionization signal
Equilized ADC counts
Not-interacting ions
30.0GeV/u
(2013 test)
Non-linear behaviour for higher Z
Courtesy of Pisa/Siena group

## Slide 20: Optical cross-talk
0.5% | 3.4% | 0.7%
3.4% | 100% | 4.0%
0.6% | 3.3% | 0.8%
0.1% | 0.5% | 0.1%
0.4% | 2.1% | 0.4%
0.1% | 0.5% | 0.2%
Layer 1
Layer 0
Feb.2013 prototype:
  Teflon wrapping + Delrin mechanical structuers
   scintillation light propagates to adjacent crystals
Optical cross-talk verified in lab with green and red led light
Feb.2015 prototype:
  Absorber film (Tedlar) added to Teflon wrapping
LED light

## Slide 21: Ionization signal –vs– Z2
O
|
F
|
Ne
|
|
Cl
O
|
F
|
Ne
|
|
Na
Ionization signal
Cross-talk signal
Equilized ADC counts
Equilized ADC counts
Linear fit from He to O
Linear fit from Na to Cl
Na
|
Non-linearity in scintillator response to high-Z ions
Non-linear behaviour for higher Z  not instrumental but physical effect
Courtesy of Pisa/Siena group

## Slide 22: Ionization signal vs Z2
17%
discrepancy
 Central crystal (gaussian fit)
 Total over layer
MC tuning:
14% optical cross talk  to match cube/layer signal ratio for C
4.5% additional gaussian spread to single-crystal signal  to match ionization-signal spread
Not-interacting ions
30.0GeV/u
(2013 test)

## Slide 23: MC model of the prototype
Fluka package
Materials:
  CsI crystals
  Si sensors (150 μm tichness)
  Kapton cables
  Delrin plates
Beam
  Gaussian, on central cube
  Monoenergetic ions (2H, 4He, 12C )
MC normalization:
  MeV  #p.e. conversion from nominal CsI and Si parameters
  #p.e.  ADC channels conversion at measured MIP signal
  Gaussian random noise from measured map  common noise extract event-by-event from data

## Slide 24: MC tuning
C ions @ 30.0GeV/u
2H @ 30.0GeV/u
14% optical cross talk  to match cube/layer signal ratio for C
4.5% additional gaussian spread to single-crystal signal  to match ionization-signal wight
Average ion.signal distribution
Cube-to-layer signal distribution

## Slide 25: Shower study

## Slide 26: Calorimeter linearity
A/Z=2 fragments from Pb+Be collisions
12.8 GeV/u
30.0 GeV/u
Shower initiating within ~5° layer
Equilized ADC counts
Courtesy of Pisa/Siena group

## Slide 27: Shower classification
Ion-beam data
30.0GeV/u
2013 test
max  AE
ion  Z2
start
Shower classified on the basis of the starting point
At least one hit with
signal > 7.5Z
At least two hits with
signal > ion+3

## Slide 28: Shower profile
Ions @ 30.0GeV/u
2013 test
Li
He
D
C
He

## Slide 29: Energy resolution –vs– shower containment
Ion-beam data
He @ 30.0GeV/u
2013 beam-test
Gaussian fit
Histogram statistics
Energy deposit (a.u.)
Energy resolution

## Slide 31: Beam-test –vs– MC data
Ion-beam data
He @ 30.0GeV/u
2013 setup
Gaussian fit
Histogram statistics
MC (Fluka)
Energy deposit (a.u.)
Energy resolution
Better than 5% agreement
Up to 15% disagreement

## Slide 32: Beam-test –vs– MC data
 Beam-test
 MC
12.8 GeV/n
30.0 GeV/n
Beam test
MC
+4%
-10%
+6%
-14%

## Slide 33: Beam-test –vs– MC data
Beam test
MC
+1%
-5%
+5%
-3%

## Slide 34: Energy resolution –vs– A
 Beam test 2013
 MC
Showers starting on layer 1
12.8 GeV/n
30 GeV/n

## Slide 35: Energy resolution –vs– A
Showers starting on layer 2
 Beam test 2013
 MC
12.8 GeV/n
30 GeV/n

## Slide 36: Energy resolution –vs– A
Showers starting on layer 3
 Beam test 2013
 MC
12.8 GeV/n
30 GeV/n

## Slide 37
Energy deposit +4%
Resolution -16%
MC
Showers starting on layer 1
He @ 30.0 GeV/n
33.8%
28.3%
beam‘-test 2013

## Slide 38: 2013 –vs– 2015 prototype
33.8%
33.5%
preliminary
(Z-tagging from first calorimeter layer )
beam-test 2015
beam-test 2013
Showers starting on layer 2
He @ 30.0 GeV/n

## Slide 39: Summary & conclusions
Beam tests
  Feb.2013  first test of 3314 prototype with ions @SPS
  Feb.2015  second test with ions @SPS
    Upgrade: optical cross talk removed by shielding the crystal with Tedlar layer
Study of detector response to ionization energy deposits
  Non-linear Z2 dependency found
  Precise characterization with 2015 data under progress
Study of shower classification and energy resolution
  MC tuned on 2013 data  agreement MC/data within 15%
  MC tuning with 2015 under progress  better MC-to-data match expected
Planned beam-test
  Aug.2015  test of the 3314 prototype with high-energy p and e @SPS
    Upgrade: Vikuiti wrapping & (if possible) small-area PDs

## Slide 40: SPARE SLIDES

## Slide 41: Channel Noise
Without common-noise subtraction
With commom- noise subtraction
CASIS
0
CASIS
1
CASIS
2
CASIS
3
CASIS
4
CASIS
5
CASIS
6
CASIS
7
CASIS
8
ADC counts

## Slide 42: MIP signal
He
CN subtracted  S/N~13.5
No CN subracted S/N~7.2
D

## Slide 43: Ionization signal relative width
Additional gaussian fluctuations (4.5%) tuned to match carbon resolution
A30GeV
NB distributions are not gaussian

## Slide 44: Direct energy deposit on photodiode
MIP
Central cube first layer
Carbon 12.8 GeV/amu
Crystal ~ 44 MIP
Crystal+sensor ~ 60 MIP
C ions traversing the photodiode

## Slide 45: Switching from high to low gain
Saturation
High gain | low gain
F
Na
He

## Slide 46: Saturation
30.0 GeV/n

## Slide 47: Saturation
12.8 GeV/n

## Slide 54: Shower starting-point distribution
4He @ 12.8 GeV/u

## Slide 55
Missing lateral
element
Missing corner
element
Ion-beam data
30.0GeV/u
2013 setup
Li
He
D

## Slide 56
Ion-beam data
30.0GeV/u
2015 setup
Missing central
And lateral element
Missing lateral
element
Missing corner
element

## Slide 57: Shower profile
C @ 30 GeV/u
C @ 12.8 GeV/u
Ion-beam data
2013 setup
Showers starting on layer 2

## Slide 58: Energy resolution –vs– A

## Slide 59
Discrepancy
+1%
-5%
Discrepancy
+5%
-3%

## Slide 60
Discrepancy
-3%
-7%
*
*
NB!

## Slide 61
Discrepancy
-2%
-8%
+1%
-5%
Discrepancy
-2%
-9%
+5%
-3%
NB!

## Slide 62
Discrepancy
0%
-11%
+2%
-5%
Discrepancy
-2%
0%
+5%
+6%
NB!
21.6%
21.5%
21.3%
21.6%
21.5%
21.3%

## Slide 63
Teflon tape 50 um
Number of layers varies from 2 (prototype config) to 16
Peak α 5,5 MeV

## Slide 66: Cube-to-layer signal fraction
Simulation vs data
Data:
Carbon beam
1230.0GeV/c
MC: noise included
Selection:
Events with maximum signal on first-layer central cube
Second layer

## Slide 67: Cube-to-layer signal fraction
Simulation vs data
Expected
cube-to-layer signal fraction 83%
Second layer
Data:
Carbon beam
1230.0GeV/c
MC: noise & OCT (20%)
Selection:
Events with maximum signal on first-layer central cube

## Slide 68: Cube-to-layer signal fraction
Simulation vs data
Cube-to-layer signal fraction forced to 88%, by modifying
Data:
Carbon beam
1230.0GeV/c
MC: noise & OCT (14%)
Selection:
Events with maximum signal
on first-layer central cube
Second layer

## Slide 69: Total number of hits
Simulation vs data
Data:
Helium beam
430.0GeV/c
MC: noise included
Selection:
Events with maximum signal on first-layer central cube

## Slide 70: Total number of hits
Simulation vs data
Data:
Helium beam
430.0GeV/c
MC: noise & OCT (14%)
Selection:
Events with maximum signal on first-layer central cube

## Slide 71: Ionization signal (average)
Data:
Deuterium beam
230.0GeV/c
MC:
noise
OCT (14%)
Gaussian spread (4.5%)
Non interacting ions selected
Single-cube signals (sensor excluded)
Cumulative distribution of all (internal) layers
p.e.-to-ADC normalization tuned to match deuterium ionization peak

## Slide 72: Ionization signal (average)
Data:
Helium beam
430.0GeV/c
MC:
noise
OCT (14%)
Gaussian spread (4.5%)
Non interacting ions selected
Single-cube signals (sensor excluded)
Cumulative distribution of all (internal) layers

## Slide 73: Ionization signal (average)
Data:
Carbon beam
1230.0GeV/c
MC:
noise
OCT (14%)
Gaussian spread (4.5%)
Non interacting ions selected
Single-cube signals (sensor excluded)
Cumulative distribution of all (internal) layers
Additional gaussian fluctuations added to match the Carbon relative width